R10 370 Dales Aluminium Rainwater Pipes in Anodised Finish
Guidance for Quantity Surveyors

As all accessories are factory manufactured, these components do need to be measured as “extra over” items within the bills of quantities.  Please contact Dales on tel: 0115 930 1521 or email techinfo@dales-eaves.co.uk for further clarification.
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R10 RAINWATER DRAINAGE SYSTEMS

370 Aluminium Pipework For External Use
Manufacturer: Dales Fabrications Ltd, Crompton Road Industrial Estate, Ilkeston, Derbyshire. DE7 4BG.  Tel: 0115 930 1521, Fax: 0115 903 7625. Email: techinfo@dales-eaves.co.uk Website: www.dales-eaves.co.uk.  The supplier shall design and manufacture the system in accordance with BS EN ISO 9001:2015 and hold Professional Indemnity Insurance to cover their design activities. The Design of the system, including components, support structure, fixings and sealant, shall accommodate typical loadings/stresses in accordance with relevant British Standards.

Product Reference: Dales Secret Fix VR Aluminium Rainwater Pipes.
Material: Extruded Aluminium to BS EN 755 Part 1, 2 & 9 2001 6063 T4: supplied by BS EN ISO 9002 registered stockist to ensure traceability and responsible sourcing.

Shape: Square
Size: 101.6mm
Gauge: 2.0mm
Finish: Anodised after fabrication to min. 25 microns to BS3987 by United Anodisers or equivalent 

Colour: 

Natural Silver

Colour Ref: UA-100A 
(Specify or delete)
Anolok Bronze™: 

Colour Ref: 

(Specify particular colour code or delete)
Anolock™ II Blue Grey: 
Colour Ref:_________ 
(Specify particular colour code or delete)
UV Dye: 


Colour ref:  UA-_____-___(Specify particular colour code or delete)
(See available anodised finishes at https://www.dales-eaves.co.uk/finish/anodised/)
Fixings: Fixings recommended for the purpose and supplied by Dales Fabrications Ltd. 

Other requirements: Secret Fix Internal Spigot joints

Accessories: Pipe connectors/square to round adapters/pipe elbows/rodding access pieces/hopper heads/pipe brackets/offset pipe brackets/pipe branches/pipe offsets/two-piece adjustable offsets/special items to be designed and factory manufactured specifically for the application.
Method of Jointing: Dry internal socket joint 

Method of Fixing: Secret Fix in accordance with manufacturer’s instructions, generally one bracket per pipe length.  All brackets to be supplied by Dales Fabrications Ltd.
